## Slide 1
Phil Murgatroyd
MPA-Q, LANL
Los Alamos Computational Condensed Matter Summer School 2026
6/22/2026
Seeing Electrons: A Pedagogical Introduction To Angle-Resolved Photoemission Spectroscopy

## Slide 2
Section 1: Emergent Phenomena
Notes: It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure , we could directly observe many-body physics.
It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure 𝐴(𝐤ⓜ,𝜔), we could directly observe many-body physics.

## Slide 3
Simple local interactions can give rise to extraordinary collective behavior
Notes: If I asked you to understand this system by tracking the trajectory of a single bird, you'd miss the point entirely. The remarkable behaviour emerges from the interactions between many individuals.
Condensed matter physics faces a similar challenge...

## Slide 4
Collective electronic behavior gives rise to emergent quantum phenomena
Superconductivity
Notes: Levitation → correlations create macroscopic order (superconductivity)
Wigner crystal → correlations localize and organize electrons (Mott/Wigner physics)
Cold atom TOF → correlations drive phase transitions (emergence of new states)

## Slide 5
Collective electronic behavior gives rise to emergent quantum phenomena
Superconductivity
Wigner Crystal
Notes: Levitation → correlations create macroscopic order (superconductivity)
Wigner crystal → correlations localize and organize electrons (Mott/Wigner physics)
Cold atom TOF → correlations drive phase transitions (emergence of new states)

## Slide 6
Collective electronic behavior gives rise to emergent quantum phenomena
Superconductivity
Wigner Crystal
Mott insulator — superfluid transition in cold atoms
Notes: Levitation → correlations create macroscopic order (superconductivity)
Wigner crystal → correlations localize and organize electrons (Mott/Wigner physics)
Cold atom TOF → correlations drive phase transitions (emergence of new states)

## Slide 7
Collective electronic behavior gives rise to emergent quantum phenomena
Superconductivity
Wigner Crystal
Mott insulator — superfluid transition in cold atoms
How do we connect these macroscopic phenomena to their microscopic origin?
Notes: Levitation → correlations create macroscopic order (superconductivity)
Wigner crystal → correlations localize and organize electrons (Mott/Wigner physics)
Cold atom TOF → correlations drive phase transitions (emergence of new states)

## Slide 8
How do we probe quantum matter?
Macroscopic Probes

## Slide 9
How do we probe quantum matter?
Macroscopic Probes
Electrical Transport

## Slide 10
How do we probe quantum matter?
Macroscopic Probes
Electrical Transport
Magnetometry

## Slide 11
How do we probe quantum matter?
Macroscopic Probes
Electrical Transport
Magnetometry
Calorimetry

## Slide 12
How do we probe quantum matter?
Macroscopic Probes
Electrical Transport
Magnetometry
Calorimetry
These measurements reveal that something unusual occurs...

## Slide 13
… but they do not tell us directly what the electrons are doing

## Slide 14
What do we really want to know?

## Slide 15
What do we really want to know?
What states exist?

## Slide 16
What do we really want to know?
What states exist?
Which are occupied?

## Slide 17
What do we really want to know?
What states exist?
Which are occupied?
How do interactions modify them?

## Slide 18
What do we really want to know?
What states exist?
Which are occupied?
How do interactions modify them?
How do they disperse?

## Slide 19
What do we really want to know?
What states exist?
Which are occupied?
How do interactions modify them?
How do they disperse?
How long do they live?

## Slide 20
What do we really want to know?
Can we directly observe the electronic degrees of freedom?

## Slide 21
The Spectral Function
The central quantity describing electronic excitations.
Notes: It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure , we could directly observe many-body physics.
It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure 𝐴(𝐤ⓜ,𝜔), we could directly observe many-body physics.

## Slide 22
The Spectral Function
The central quantity describing electronic excitations.
Encodes:
Where electronic states exist
Their momentum
Their lifetime
Their spectral weight
Notes: It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure , we could directly observe many-body physics.
It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure 𝐴(𝐤ⓜ,𝜔), we could directly observe many-body physics.

## Slide 23
The Spectral Function
The central quantity describing electronic excitations.
Encodes:
Where electronic states exist
Their momentum
Their lifetime
Their spectral weight
If we could measure, we could directly observe many-body physics.
Notes: It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure , we could directly observe many-body physics.
It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure 𝐴(𝐤ⓜ,𝜔), we could directly observe many-body physics.

## Slide 24
Section 2: The ARPES Experiment
Notes: It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure , we could directly observe many-body physics.
It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure 𝐴(𝐤ⓜ,𝜔), we could directly observe many-body physics.

## Slide 25: ARPES: General Description
ARPES exploits the kinematics of the photoemission process to:

## Slide 26: ARPES: General Description
ARPES exploits the kinematics of the photoemission process to:
deduce the binding energy

## Slide 27: ARPES: General Description
ARPES exploits the kinematics of the photoemission process to:
deduce the binding energy
crystal momentum
of the electron before it was emitted from the material

## Slide 28: ARPES: Experimental Process
Irradiate a single-crystal sample with monochromatic light of energy

## Slide 29: ARPES: Experimental Process
Irradiate a single-crystal sample with monochromatic light of energy
Collect photoelectrons in spectrometer

## Slide 30: ARPES: Experimental Process
Irradiate a single-crystal sample with monochromatic light of energy
Collect photoelectrons in spectrometer
Record the kinetic energy and emission angles

## Slide 31: ARPES: Conservation Laws
Notes: In-plane momentum is conserved throughout the photoemission process due to in-plane periodicity modulo an inplane reciprocal lattice vector… the orthogonal component is not conserved

## Slide 32: ARPES: Conservation of Energy

## Slide 33: ARPES: Momentum Conservation

## Slide 34: ARPES: Experimental Setup
Performed in ultra high-vacuum environments (<10-10 mbar)
At cryogenic temperatures (<15 K)
Multi-axis manipulator
Detectors are hemispherical analyzers
Can use a range of light sources such as:
Lasers (6 – 11 eV)
Plasma sources (21-40 eV)
VUV synchrotrons (20-200 eV)
Soft- Xray synchrotrons (400-1000 eV)

## Slide 35: ARPES: ARPES Measurements
2d dispersions

## Slide 36: ARPES: ARPES Measurements
3d maps
2d dispersions

## Slide 37
Section 3: ARPES Formalism
Notes: It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure , we could directly observe many-body physics.
It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure 𝐴(𝐤ⓜ,𝜔), we could directly observe many-body physics.

## Slide 38: ARPES: Fermi’s Golden Rule

## Slide 39: ARPES: Fermi’s Golden Rule
Formally:
Photoemission process described by transition probability
N-electron initial state to an excited final state

## Slide 40: ARPES: Fermi’s Golden Rule
Formally:
Photoemission process described by transition probability
N-electron initial state to an excited final state
is a perturbative Hamiltonian describing the electron-photon interaction

## Slide 41: ARPES: Three-step model

## Slide 42: ARPES: Three-step model
Photon drives a direct optical transition for an electron in the bulk of the material. This step contains the information on the intrinsic electronic structure of the material.

## Slide 43: ARPES: Three-step model
Photon drives a direct optical transition for an electron in the bulk of the material. This step contains the information on the intrinsic electronic structure of the material.
Electron propagates to the surface. This process is described in terms of an effective mean free path λMFP imposed by both elastic and inelastic scattering processes.

## Slide 44: ARPES: Three-step model
Photon drives a direct optical transition for an electron in the bulk of the material. This step contains the information on the intrinsic electronic structure of the material.
Electron propagates to the surface. This process is described in terms of an effective mean free path λMFP imposed by both elastic and inelastic scattering processes.
Electron is transmitted through the surface barrier, with the electron occupying a free-electron plane wave state in the vacuum extending to the detector.

## Slide 45: ARPES: Three-step model (step 1)
Consider a non-interacting system:
Invoke the Sudden approximation
The N-electron initial and final states are given by
Where A is an anti-symmetry operator enforcing the Pauli principle
and are wave function of the electron before and after absorbing a photon
Both have same wave vector k due to momentum conservation
They have energies and
The non-interacting limit says that the (N-1) system is unaffected by the removal of one electron --- thus is equal to

## Slide 46: ARPES: Non-interacting photocurrent
If we calculate the total photocurrent:
Plugging approximations into:
Assuming a single transition (i->f) at each k
We recover:

## Slide 47: ARPES: Non-interacting photocurrent
ARPES spectrum of a noninteracting system is:
- a sharp peak that traces the electronic band dispersion ϵk
- with its intensity modulated by the dipole matrix element.
This result establishes the capability of ARPES to be used as a band-mapping technique

## Slide 48: ARPES: Single-particle spectral function

## Slide 49: ARPES: Single-particle spectral function
Description valid near the Fermi surface with the conditions for small .

## Slide 50: ARPES: Single-particle spectral function
This is what elevates ARPES from being a band-structure camera to a many-body spectroscopy

## Slide 51: ARPES: Three-step model (step 2)

## Slide 52: ARPES: Three-step model (step 3)

## Slide 53: ARPES: Advantages and Limitations

## Slide 54
Section 4: Real Examples
Notes: It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure , we could directly observe many-body physics.
It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure 𝐴(𝐤ⓜ,𝜔), we could directly observe many-body physics.

## Slide 55: Class: Topological Materials
ARPES is ideally suited for studying 2-dimensional materials

## Slide 56: Class: Topological Materials
ARPES is ideally suited for studying 2-dimensional materials
The interest in low-dimensional topological materials in the 2010s came at a perfect time for ARPES

## Slide 57: Class: Topological Materials
ARPES is ideally suited for studying 2-dimensional materials
The interest in low-dimensional topological materials in the 2010s came at a perfect time for ARPES
Type-II Dirac Semimetal PtSe2

## Slide 58: Class: Topological Materials
ARPES is ideally suited for studying 2-dimensional materials
The interest in low-dimensional topological materials in the 2010s came at a perfect time for ARPES
In some ways one can think of this close the non-interacting limit and why vanilla DFT does so well
Type-II Dirac Semimetal PtSe2

## Slide 59: Class: Correlated Transition Metal Oxides
Layered Ruddlesden-Popper Sr2RuO4 presents: -highly-anisotropic transport behavior
-enhanced effective masses

## Slide 60: Class: Correlated Transition Metal Oxides
Layered Ruddlesden-Popper Sr2RuO4 presents: -highly-anisotropic transport behavior
-enhanced effective masses

## Slide 61: Class: Correlated Transition Metal Oxides
Layered Ruddlesden-Popper Sr2RuO4 presents: -highly-anisotropic transport behavior
-enhanced effective masses
Highly 2d Fermi surface
Kinks in dispersions and reduced Fermi velocities showing
correlation effects

## Slide 62: Class: Correlated Transition Metal Oxides
Fermi surface can be recovered by LDA calculations…

## Slide 63: Class: Correlated Transition Metal Oxides
Fermi surface can be recovered by LDA calculations…
We need LDA+U to recover the renormalization of the bands

## Slide 64: Class: Heavy Fermion Compounds
Formation of heavy bands in CePd3 cannot be described by DFT

## Slide 65: Class: Heavy Fermion Compounds
Formation of heavy bands in CePd3 cannot be described by DFT
Reproducing the shift in spectral weight due to the coherent Kondo lattice formation requires higher level theory such as DMFT

## Slide 66: Class: Heavy Fermion Compounds
Formation of heavy bands in CePd3 cannot be described by DFT
Reproducing the shift in spectral weight due to the coherent Kondo lattice formation requires higher level theory such as DMFT

## Slide 67
Section 5: Technological Advances
Notes: It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure , we could directly observe many-body physics.
It tells us:
Energy
Momentum
Lifetime
Spectral weight
If we could measure 𝐴(𝐤ⓜ,𝜔), we could directly observe many-body physics.

## Slide 68: Advancement: Spatially-resolved ARPES
Development of spot-sizes below 10 microns allows for samples to be spatially profiled We can now study heterostructure stacks as well as disparate terminations on cleaved samples
Delafossite
PdCoO2

## Slide 69: Advancement: Spin-resolved ARPES
Spin-resolved ARPES allows us to directly visualize momentum-locked spin textures in a range of material classes
Rashba-split surface state in Au(111)

## Slide 70: Advancement: Time-resolved ARPES
Time-resolved (tr)-ARPES allows one to characterize the nonequilibrium properties of quantum materials
Pump-probe technique
Can allow one to probe the dynamics for a range of quantum materials

## Slide 71: Conclusions

## Slide 72: Conclusions
ARPES provides direct access to electronic excitations
By measuring energy and momentum simultaneously, ARPES experimentally accesses the occupied spectral function.

## Slide 73: Conclusions
ARPES provides direct access to electronic excitations
By measuring energy and momentum simultaneously, ARPES experimentally accesses the occupied spectral function.
ARPES is not a band-structure camera
It is a many-body spectroscopy sensitive to:
Renormalization
Spectral-weight transfer
Quasiparticle lifetimes
Collective electronic behavior

## Slide 74: Conclusions
ARPES provides direct access to electronic excitations
By measuring energy and momentum simultaneously, ARPES experimentally accesses the occupied spectral function.
ARPES is not a band-structure camera
It is a many-body spectroscopy sensitive to:
Renormalization
Spectral-weight transfer
Quasiparticle lifetimes
Collective electronic behavior
ARPES and modern electronic structure theory form a powerful feedback loop
DFT → DFT+? → DMFT ↔ ARPES
Together they provide a microscopic understanding of quantum materials.

## Slide 75: Conclusions
ARPES provides direct access to electronic excitations
By measuring energy and momentum simultaneously, ARPES experimentally accesses the occupied spectral function.
ARPES is not a band-structure camera
It is a many-body spectroscopy sensitive to:
Renormalization
Spectral-weight transfer
Quasiparticle lifetimes
Collective electronic behavior
ARPES and modern electronic structure theory form a powerful feedback loop
DFT → DFT+? → DMFT ↔ ARPES
Together they provide a microscopic understanding of quantum materials.
You calculate .
We measure .

## Slide 76: Good References
https://link.aps.org/accepted/10.1103/RevModPhys.93.025006
https://journals.aps.org/rmp/abstract/10.1103/RevModPhys.93.025006
https://iopscience.iop.org/article/10.1238/Physica.Topical.109a00061
https://journals.aps.org/rmp/abstract/10.1103/RevModPhys.96.015003
https://iopscience.iop.org/journal/2516-1075/page/ARPES-topological-materials